## Slide 1: Magnetic Ordering on Topological Crystalline Insulator Surfaces
Part 1. 3D topological insulators and their surface states
Part 2. Ordering on the surface of magnetically doped TCI’s
Part 3. Domain walls and speculations
Sahinur Reja - Indiana
Luis Brey – CSIC, Madrid
Shixiong Zhang - Indiana

## Slide 2
3D Topological Insulators
Paradigm: Bi1-xSbx
Projection of time-reversal invariant points onto surface
guaranteed to be doubly degenerate (“Kramer’s doublet”)
Away from these points states repel ⇒ surface Dirac cone
From Hassan and Kane, RMP (2010)
Gapless nature of surface states robust: protected by
time-reversal symmetry
I. Surface states protected by time-reversal symmetry
“Surface Brillouin zone”:

## Slide 3
Model Hamiltonian for Bi2Se3 (Zhang et al. 2009):
(111) surface
Four relevant orbitals at Γ point:
(Figs from Zhang et al., Nat. Phys. 2009)
Hybridized pz orbitals of basis atoms
To consider a surface ⊥ to Γ-z, start with kz =0. In vicinity
of point:

## Slide 4
Mutually anticommuting, like Pauli matrices
Coefficients may represent 3D vector components
of k – dependent “Zeeman” Hamiltonian
For M0B2 > 0, the origin is enclosed ⇒ Topological insulator
So gapless surface states can be constructed.
Can do so explicitly with this form of H.
[Liu et al. (2010); Silvestrov et al. (2012), Brey and HAF (2014)]

## Slide 5
Example:
Rectangular slab in a magnetic field
(Brey and HAF, PRB 2014)
Lateral surface
Perpendicular surface
2. For thicker slabs, M left-movers, M+1 right movers
 Need disorder or dephasing to get correct Hall quantization
Observations:
EF
For narrow slab, can get ν = 1 QHE from
two surfaces with Landau levels
σxy= (1/2)e2/h per surface
EF

## Slide 6
Paradigm: Sn1-xPbxTe
Surface states protected by mirror symmetry
II. Surface states protected by crystalline symmetry:
Topological crystalline insulators (TCI)
(Liang Fu, MIT)
Semiconductors, “standard model” has 12 orbitals
Direct gaps at L points (4 of these)
L points are special:
1. Hnn(k=L) = 0  Sublattice a good quantum number
2. Γ – L direction hosts 3-fold rotational symmetry
3. Γ – L direction hosts 3 mirror planes
Pb/Sn sites have effectively adjustable on-site energies
controlled by x: “virtual crystal approximation”
 System can be adjusted through topological transition!

## Slide 7
Continuum bulk Hamiltonian near L point with Γ – L perpendicular to (111) surface:
BZ face perpendicular to k1
q1
q2
q3 out
τ acts on sublattice; acts on C3 eigenstates
carries out a mirror reflection across x = y plane
Set q3 = 0 and note mutually anticommute
 H1(q1, q2,0) encloses origin in this spinor space if m
⇒ possible to construct gapless surface states
Projection of H1(q) onto these states to linear order:
Surface states at
points as well,
energies <
 4 Surface Dirac cones! (Hsieh et al, 2012)

## Slide 8
Confirmation in ARPES …
(Polley et al., 2014)
… and tight binding calculations.
E/t

## Slide 9
Magnetic Impurities and Magnetism in TCI Systems
(Sn,Pb)Te doped with sufficient magnetic impurity (Mn,Eu) concentration long-known to be ferromagnetic
Impurities substitute for (Sn,Pb)
Hole-doped semiconductors: impurity
spins interact with bulk carriers holes via
ferromagnetic exchange
Story et al, 1990
If conduction electrons removed (e.g., compensation doping), impurity spins become decoupled and no magnetism. But if the system is a TCI, what happens at the surface?
EF
Levels repel if mirror symmetry breaks

## Slide 10
Mean-field approach: suppose impurity spins are uniformly polarized: constant
a1, a2, proportional to components of perpendicular to Γ – L direction
b3 proportional to component of along Γ – L direction
A,B have expressions in terms of tight-binding parameters
η = 2 anisotropy factor for surface Dirac points
Gaps of size 2b3 open at Dirac points: Mirror symmetry broken by
 Lowering of total electronic energy by a surface magnetization
Favored direction is a competition among different surface Dirac points.
Depends on chemical potential

## Slide 11
Numerical Simulations: Total energy calculations
Tight-binding model of (Sn,Pb)Te slab with (111) faces
Superlattice of localized field only on a sites, chosen near surface so that coupling to two surface states is the same
No field in bulk
(111) face
“along ”
“along ”
E

## Slide 12
EF~
EF~
Fixed N
Fixed µ
All same within a layer.
Total (free) energy computed for different orientations
h =
Free difference between and orientations
on 2/9 of sites
So direction of magnetization can be manipulated using an electric gate!
+
+
+
+
+
+
-
-
-
-
-
-

## Slide 13
Checking ferromagnetism: Does energy increase when spins not aligned?
1. Numerical (spin stiffness at short distance)
2. Perturbation theory (long distance)
Consider a generic gapped Dirac surface Hamiltonian (ignore anisotropy)
Components of proportional to components of magnetization
Consider a spatial variation: ,
Compute change in electronic energy ΔE to second order in h
What is the Q dependence for small Q (quadratic order)?

## Slide 14
Fermi surface present, result is independent of Q!
 Impurity spins are “floppy”
(b) When EF is in the gap,
Two situations:
EF
EF
Δ(0)
.
Compare to graphene spin susceptibility χ(Q) (Brey, HAF, Das Sarma, PRL 2007)
(1) For µ in-band, χ(Q) independent of Q for small Q
(2) For Q at Dirac point, χ(Q) ~ Q ⇒ 1/r3 RKKY interaction
Because Δ(0) ~ along Γ – L direction, impurity spins become stiff as system thermally disorders at high T!
As Δ(0)  0, spin-spin interaction becomes long-ranged

## Slide 15
III. Domain Walls and Thermal Disordering
Simple model of surface magnetization : (appropriate spin stiffness)
Number of energy minima
From zero-field cooling or in thermal equilibrium
Look for effects of increased conduction: tunneling, surface conductance, surface reflectance
ΔC1 = 1: Jackiw-Rebbi mid-gap
states
Number of channels depends on how many b3’s change sign: Up to 4 possible!
e.g., two-fold symmetry
Δ(0) ~ b3
Δ(0) ~ -b3
C1 = 1/2
C1 = -1/2

## Slide 16
Domain Walls for TCI:
Use surface states of un-magnetized as basis
Project into this space, with
a domain wall configuration
3. Diagonalize projected Hamiltonian
a good quantum number
a good quantum number
4. Periodic b.c. ⇒ two DW’s per unit cell, per surface
Example: ‖ (111) → : ‖ - (111)
⇒ 4 b3’s change direction
Expect 4 x 4 in-gap states

## Slide 17
Does the presence of in-gap states change the long-range interaction? No.
3-d Coulomb-like interaction among spin gradients.
Numerical evidence from graphene:
DW’s in staggered magnetization
Δ0
x
L
DW
DW
Expect logarithmic interaction!
µ in gap
µ in gap
µ in band
µ in band

## Slide 18
1.
µ above and :
µ
Low T → Ising order
DW’s: finite energy
per unit length
2.
µ ~ , above :
µ
Low T → Ising order
Stiffness consistent with
a long-range Ising model
⇒ Thermal disordering
transition in Ising class
⇒ Thermal disordering
transition with
mean-field exponents
[M.F. Paulos et al., Nuc. Phys. B (2016)]

## Slide 19
For µ~, there are six degenerate directions for ferromagnetic order.
Is this a six-state clock model, or two coupled three-state models?
Check the domain walls energies!
ΔE = E(L2 →L3)- E(L2 →L1)
always negative
⇒ six-state model
S = 0.01t
S = 0.1t

## Slide 20
3.
µ below , µ~:
µ
Low T → broken 6-fold symmetry
Stiffness consistent with
a long-range Ising model
⇒ Thermal disordering
transition with
mean-field exponents?
4.
µ band :
µ
Low T → broken 6-fold symmetry
DW’s: finite energy
per unit length
⇒ Thermal disordering
transition in
Kosterlitz-Thouless class
[Jose et al., 1977]

## Slide 21
Sahinur Reja - Indiana
Luis Brey – CSIC, Madrid
Shixiong Zhang - Indiana
Funding:
Many thanks to …

## Slide 23
Summary
Topological crystalline insulator offers hosts gapless surface states protected
by mirror symmetry.
Model of surface states can be formulated, allowing access to explicit forms
of surface wavefunctions.
3. Magnetic dopants may order to break the symmetry, lowering total electronic
energy. Specific low energy orderings depend on chemical potential and
specific surface: 2-fold and 6-fold orderings likely to occur on (111) surface.
Long-wavelength stiffnesses sensitive to chemical potential: impacts energetics
of domain walls and yields many types of thermal disordering transitions, all in a
single system!
Thank you!!
Sahinur Reja, HAF, Luis Brey, and
Shixiong Zhang, PRB 96, 201111 (R) (2017)